[image: image1.wmf]Min

Nom

Max

Max

Min

Nom

Max

ACF-351 275

13 µm

261

275

289

<0,06

0,45

0,65

0,85

ACF-351 300

13 µm

285

300

315

<0,06

0,45

0,65

0,85

ACF-351 600

13 µm

570

600

630

<0,06

0,45

0,65

0,85

ACF-351 900

15 µm

810

900

990

<0,06

0,40

0,55

0,70

ACF-351 1200

17 µm

1080

1200

1320

<0,06

0,40

0,55

0,70

ACF-351 2400

17 µm

2160

2400

2640

<0,06

0,40

0,55

0,70

ACF-351 4800

24µm

4320

4800

5280

<0,06

0,45

0,6

0,75

Loss of ignition                           

(%)

Filament 

diameter

References

Linear density                   

mass in g/km

Moisture 

content (%)

DIRECT ROVING 




ACF-351 
Taiwan Glass Ind. Corp.
PROPertieS


( Very low fuzz
( Fast wet out
( Good processing characteristics

( Low catenary

( Good handling characteristics

( High mechanical properties

ACF-351 Roving is an untwisted, single end roving, supplied as a tubeless package, for use in continuous process operations, such as weaving, pultrusion and filament winding. The sizing is specifically designed for fast wet out, good processing and handling characteristics as well as 

excellent adhesion with most Polyester, Vinyl Ester and Epoxy resins.
SPECIFICATIONS



[image: image3.png]i




PACKAGING 


Each individual cheese is contained within a transparent shrink wrap bag.


[image: image2.wmf]Pallet

Net weight (kg)

48  /  64

864  /  1152

Cheese per 

pallet

20 ' container

20

20 160

Net weight per 

pallet (kg)

Reference

Weight per 

cheese (kg)

ACF-351

18


STORAGE


Our roving ACF-351 should be stored dry in its original packaging.
Storage temperature : 21+/-11 °C – Relative moisture : 60 +/-20%
Glass fiber products must remain in packaging material  just prior to its use.
It is recommended to bring material in the working place 24 hours at least prior to use.
FRP Services Europe reserves the right to change the information given herein without prior notice. We believe this information to be reliable, but do not guarantee its applicability to the user’s process or assume liability for occurrence arising out of its use. The user, by accepting products described herein agrees to responsible for thoroughly testing any application before committing to production.


JANUARY 2010








_1374648653.xls
Feuil1

		References		Filament diameter		Linear density                   mass in g/km						Moisture content (%)						Loss of ignition                           (%)

						Min		Nom		Max		Min				Max		Min		Nom		Max

		ACF-351 275		13 µm		261		275		289		18,432				<0,06		0.45		0.65		0.85

		ACF-351 300		13 µm		285		300		315						<0,06		0.45		0.65		0.85

		ACF-351 600		13 µm		570		600		630		18,432				<0,06		0.45		0.65		0.85

		ACF-351 900		15 µm		810		900		990						<0,06		0.40		0.55		0.70

		ACF-351 1200		17 µm		1080		1200		1320		18,432				<0,06		0.40		0.55		0.70

		ACF-351 2400		17 µm		2160		2400		2640						<0,06		0.40		0.55		0.70

		ACF-351 4800		24µm		4320		4800		5280						<0,06		0.45		0.6		0.75






_1326202881.xls
Feuil1

				Poids des Pelotes ( kg )		Pelotes par Palettes		Poids par Palette ( kg )						Humindité (%)

		Reference		Weight per cheese (kg)		Cheese per pallet		Net weight per pallet (kg)		20 ' container				0.15

										Pallet		Net weight (kg)

												(kg)

		ACF-351		18		48  /  64		864  /  1152		20		20,160






